## Slide 1
Applying Systematic Risk Management Protocol to the Design of a Modern Propellant Manufacturing Plant in Australia Bob Ford
rford@smsenergetics.com
www.smsenergetics.com
August 2018

## Slide 2: Presentation Outline
Mulwala Redevelopment Project (MRP) introduction
SMS Approach:
  Systematic Risk Assessment
  In-Process Characterization & Classification Testing
  Applying Test Data to Minimize Risk
Summary

## Slide 3
MRP Introduction

## Slide 4: Mulwala Redevelopment Project (MRP) - ADoD

## Slide 5: Mulwala Redevelopment Project
An Australian Department of Defence contract to design, construct, commission, and qualify a 530 tonnes per year single-base propellant process plant. Upgrading the munitions factory that was built in the 1940’s to support World War II.
25mm Propellant
556 Blank Propellant
BS-NACO Propellant
.50 Cal Ball Propellant
556 Ball Propellant

## Slide 6: MRP Team
Lend Lease – Prime
ATK – Technology Provider
SMS – 3rd Party Explosives Safety

## Slide 7: MRP Requirements
Improved Safety
Modern/Enhanced Propellant Manufacturing
No Possibility of 1.1 Events
  1.3 Maximum Potential Event
Continued Propellant Production during Construction
Regulatory Compliance during and after MRP Construction

## Slide 8: MRP Team: Risk Management Philosophy
“Safety by Design”
  Minimize Personnel Exposure
  Minimize Quantities of Hazardous Materials
  Safety Specifications
Standards
Procedures
Training

## Slide 9: SMS Stewardships
Systematic Risk Assessment
Explosives In-Process Characterization & Classification Testing
Facility Siting
  Site Plans
  Concurrent Operations
  Facility Design Specifications
  Barricade Design
  Workstation Protection
Regulatory Compliance
Explosives Test Equipment
Training

## Slide 10: Relationship of Risk Assessment to Proper Classification of Explosives
Key Parameters:
Composition
Physical State
Configuration/Confinement
Conditions
Explosives Characterization Tests
Risk Assessment
Explosives Classification
Process
Equipment Design
Control System Design
Attended vs. Remote
Risk Acceptance
Facility:
Site Plan
Concurrent Operations
Facility Design
Barricades

## Slide 11
SMS Approach:
  Systematic Risk Assessment
  In-Process Characterization & Classification Testing
  Applying Test Data to Minimize Risk

## Slide 12: Elements of a Successful Risk Management Program

## Slide 13: What Creates the Need for Systematic Risk Assessment and “In-Process” Characterization/Classification?
Simple to Complex Systems/Processes
Multitude of potential scenarios
Variations in energetic material
  Compositions
  Physical States
System insult energies (normal & abnormal)
Variable process configurations and confinement

## Slide 14: Processes and Unique Hazards

## Slide 15: Key Parameters for Explosives
 | Manufacturing | Storage | Transport | Use
Composition | Variable | Constant/ Variable | Constant | Constant/ Variable
Physical State | Variable | Constant | Constant | Constant/ Variable
Configuration/ Confinement | Variable | Constant/ Variable | Constant | Variable
Quantity | Variable | Constant/ Variable | Constant | Variable
Conditions | Variable | Variable (Bounded) | Variable (Bounded) | Variable
Initiation Stimulus | Variable | Variable (Bounded) | Variable (Bounded) | Variable

## Slide 16
Transport
Life Cycle Stages of Explosives
Storage
(Configured for Transport)
4
6
7
9
10
12
1
5
2
13
General Industry
Use/Application
Configured for Transport
Processing
Research & Development
Waste, Reuse, or Recycling
Remanufacturing
Intermediate Storage
3
Manufacturing
Processing/
Operations
Explosive Industry
Use/Application
Display/Access
8
11
Service Magazine
General Industry
Warehouse/Stock Room
Explosive Industry Magazine
Removed from
Transport Configuration

## Slide 17
Identify Potential Hazards Based on
Normal and Abnormal Events and Causes
  Insult Energies
  Configurations
  Conditions
Organize by Operational Steps
OR Process Equipment
Perform Explosives Testing
that Simulates In-Process:
  Insult Energies
  Configurations
  Conditions
Test Data in
Energy Units
Insult Energies
Determined by
  Measuring
  Calculating
  Modeling
Recommend Risk Mitigating Measures
  Equipment Specifications
  Operating Parameters
  Facility Design/Shielding
  Etc.
Existing
Safeguards
Explosives Risk Assessment
Key for MRP
Evaluate/Assess Risk
  Qualitative
  Quantitative

## Slide 18
SMS Approach:
  Systematic Risk Assessment
  In-Process Characterization & Classification Testing
  Applying Test Data to Minimize Risk

## Slide 19: MRP Application of “In-Process” Characterization & Classification Tests
Sensitivity Testing
  Friction Sensitivity Test
  Impact Sensitivity Test
  ESD Sensitivity Test
  Thermal Tests (SBAT)
Reactivity Testing
  Critical Height
  No. 8 Cap Sensitivity Test
  NOL Card Gap Test
  Small Scale Burn
  etc.
Subscale, Bench-scale and full-scale simulation tests

## Slide 20: Friction Sensitivity Test (ABL)
Units: N/m2
Force/area
@ velocity

## Slide 21: ESD Sensitivity Test (ABL)
E=½CV2
E=½QV
Units: Joules

## Slide 22: Impact Sensitivity Test (MBOM)
Energy/Area
Units: J/m2

## Slide 23: Log Logistic Regression Plot (Characteristic Curve)
Chart: Impact Energy, J/m2
| 12077.457613411252 | 16053.419102110705 | 20027.097596426185 | 24980.717111825259 | 31879.782300613751
Data | 0.034 | 0.1 | 0.3 | 0.4 | 0.6
Log Logistic Fit | 5.5322e-19 | 1.4235e-05 | 0.0005659 | 0.0014832 | 0.0057506 | 0.014947 | 0.031066 | 0.055787 | 0.090133 | 0.1342 | 0.18703 | 0.24671 | 0.31074 | 0.37638 | 0.44112 | 0.50296 | 0.56049 | 0.6129 | 0.65988 | 0.70149 | 0.73802 | 0.76988 | 0.79758 | 0.82159 | 0.8424 | 0.86043 | 0.87607 | 0.88966 | 0.90148 | 0.91179 | 0.92081 | 0.92871 | 0.93565 | 0.94177 | 0.94718 | 0.95197 | 0.95622 | 0.96001 | 0.96339 | 0.96642 | 0.96913 | 0.97157 | 0.97377 | 0.97576 | 0.97755 | 0.97918 | 0.98067 | 0.98202 | 0.98325 | 0.98437 | 0.9854 | 0.98634

## Slide 24: In-Process Energies verses Material Response Data
Range of In-Process Energies
Range of Energetic Material Response
Probability
Increasing Energy Level
Chart: 
| Category 1 | Category 2 | Category 3 | Category 4
Series 3 | 2 | 2 | 3 | 0.5
Series 4 | 2 | 2 | 3 | 1
Series 5 | 2.4 | 1 | 1.8 | 0.5
Series 32 | 1 | 2 | 3 | 1

## Slide 25: Thermal Sensitivity Test (SBAT) Simulated Bulk Auto-ignition Temperature

## Slide 26: SBAT Applications
Determination of conservative auto-ignition temperature (bulk AIT value)
Determination of time to ignition at temperatures below AIT (isothermal run mode)
Conservative compatibility testing
Thermal Stability Testing
  Safe: Minimized exposure)
Complete vacuum thermal stability (with upgrade)
Notes: Talk about scale-up

## Slide 27: DSC, SBAT, and ARC AIT Temperatures
Notes: Note: the temperature at which the SBAT exotherm is reported is when the temperature deviated by greater than 1.1°C above the baseline; the DSC temperature reported is the onset temperature (point of intersection of a line drawn tangent to the steepest slope of the curve with the baseline). The ARC temperatures were determined using a “heat-wait-search” scheme while heating at an approximate rate of 0.1°C/min. The DSC and SBAT samples were heated at a constant 10°C/min and 0.22°C/min, respectively. Average deviation from ARC for SBAT and DSC is +8.6°C and +57°C respectively.

## Slide 28: Critical Height Testing
  Fastest burning Propellants tested
  Worst case geometry determined to be a 1 to 1 ratio of diameter to height

## Slide 29: Bulk Confined Sonotube™ Testing
Bulk Confined Sonotube™ testing
  Excess confinement of bulk propellant
  Larger Scale Critical Height
  Surrounded by Sand bags 295kg per pallet
  254mm diameter (10in) (concrete forming tube)
  Limit: 700mm bed depth & 600mm head space
In Process Applications
  Validation of small scale critical height results
  Ribbon blender
  Propellant Dryer
  Feed hoppers
  Bulk bag configuration in storage magazines
  Storage and transport containers

## Slide 30: Process Simulation Modeling
Blast Modeling on select equipment using Integrated Violence Model (IVM)
Inputs to model: characteristics determined by testing of propellants
Verification of designs
  Dryer
  Ribbon blender

## Slide 31: Process Example Propellant Feeder
Safeguards based on test data
  Steel hopper changed to a venting canvass hopper due to confinement
  Steel parts such as screw, chute and discharge disk changed to a plastic due to friction and impact stimulus
  Plastics tested to ensure ESD within safe limits
  Max fill of a 1:1 ratio of diameter to height (critical height) with additional level controls & interlock
  Speed of screw limited to reduce friction and impact stimulus

## Slide 32: Process Example Propellant Feeder

## Slide 33: Testing Video Propellant Feeder

## Slide 34: Process Example Propellant Feed Hopper
Receiving vessel from glazing ribbon blender
Holds up to 600kg of glazed propellant
Design based on previous testing performed by Australian Munitions on blending hopper
  Angle of hopper sides
  Size of original canvas vent and feed chute

## Slide 35: Testing Video Propellant Hopper

## Slide 36
SMS Approach:
  Systematic Risk Assessment
  In-Process Characterization & Classification Testing
  Applying Test Data to Minimize Risk

## Slide 37: Elements of a Successful Risk Management Program

## Slide 38: Summary
Accurate & Systematic Risk Assessment is “KEY” to:
  Identifying normal and abnormal process energies and process conditions
  Identifying proper sensitivity & reactivity testing and testing parameters
In-Process Sensitivity and Reactivity Testing coupled with Risk Assessment provide proper Design Specifications for:
  Process equipment
  Control Systems
  Facility Siting
  Manufacturing Facilities, Barricades, Shielding…

## Slide 39: Summary
Systematic Risk Assessment, Testing, and Management Systems Work!
MRP Design, Construction, & Qualification Completed
    2.8 Million Man Hours without LTI (1089 Days)
    No explosive events